## Slide 1
Characterizing Structural and Thermal Properties of Nb4C3Tx MXenes
Jianna Evans2, Nisha H. Makani1, Bhoj Gautam1
1Department of Chemistry, Physics and Materials Science, Fayetteville State University, Fayetteville, North Carolina 28301, United States
2Department of Mathematics and Computer Science, Fayetteville State University, Fayetteville, North Carolina 28301, United States
Figure 4. Morphology and elemental analysis of (Mo2/3Er1/3)2AlC MAX phase and (Mo2/3Er1/3)2C MXene
Summary
References
[1] L. Verger et. al., Curr. Opin. Solid State Mater. Sci., 23 (2019) 149-163.
[2] M. Khazaei et. al., Phys. Rev. Mater., 2 (2018) 074002.
[3] Y. Gogotsi, B. Anasori, ACS Nano. 13 (2019) 8491-8494.
[4] W. Wang et. al., Science. 379 (2023) 1242-1247.
Raman spectra show significant peaks at ~300 and 677 cm-1 belonging to Nb-O and Nb-C respectively. TGA was utilized to measure thermal stability, oxidation analysis, and degradation behavior by monitoring the critical change in weight percentage. DSC measurements indicate no significant thermal events up to 300°C during heating and cooling cycles. Overall, this analysis aims to contribute to the information database of properties to extend the possible applications of Nb4C3TX. This comprehensive analysis provides valuable insights into the structural and thermal behavior of Nb4C3TX MXenes, contributing to the knowledge base necessary for their potential application in high-temperature and oxidation-sensitive environments.
Contact Information:
Dr. Bhoj Gautam, Department of Chemistry, Physics and Materials Science
Fayetteville State University, Fayetteville, NC-28301
Email: bgautam@uncfsu.edu, Phone: 910-672-1653
a
b
a
b
Introduction
Abstract
XRD and Raman Analysis
Nb-based MXenes, such as Nb4C3Tx, exhibit high electrical conductivity, making them well-suited for energy storage and electronic applications. However, the greater stability of Nb-based MAX phases poses challenges in the etching and, consequently, is difficult to prepare as MXenes. Additionally, Nb-based MXenes are highly susceptible to oxidation, altering their fundamental properties. In this study, we focus on Nb4C3Tx MXenes, investigating their structural and thermal properties using (X-ray diffraction) XRD, (scanning electron microscopy) SEM, Raman spectroscopy, (Thermogravimetric analysis) TGA, and (Differential scanning calorimetry) DSC measurements. Thermal analysis plays a crucial role in determining materials' structural integrity and potential applications under high-temperature conditions. Overall, this analysis aims to contribute to the information database of properties to extend the possible applications of Nb4C3TX. This comprehensive analysis provides valuable insights into the structural and thermal behavior of Nb4C3TX MXenes, contributing to the knowledge base necessary for their potential application in high-temperature and oxidationsensitive environments. The findings aim to expand the scope of Nb-based MXenes for future technological advancements.
Sample Synthesis
Mild etching method
7 days at 70°C
Constant stirring
Oil bath
The resulting products were washed using HCl and deionized water, and vacuum dried at 70 0C to remove any solvent residue.
Figure 2. Chemical structure of (Nb4AlC3)2AlC MAX phase and (Mo2/3Er1/3)2C Mxene. −F is a functional group introduced after LiF/HCl etching.
DSC and TGAAnalysis
Figure 3. XRD patterns of (Mo2/3Er1/3)2AlC MAX phase and (Mo2/3Er1/3)2C MXene. The vanishingly small 39 peak indicates the successful removal of Al from (Mo2/3Er1/3)2AlC MAX phase. The broadening of the (Mo2/3Er1/3)2C MXene peaks indicate that
the MXene is amorphous. The shifting of the (002) peak to lower values indicates an increase in the interlayer separation (c-parameter).
Acknowledgements
The synthesis of Nb4C3Tx MXene and characterization work was supported by DOE BES-RENEW award number DE-SC0024611.This work was also partly supported by NSF RIA EES 1800795 for MXene synthesis.
(Mo2/3Er1/3)2AlC
(Mo2/3Er1/3)2C
Etching
Figure 1. These are the practical applications for Nb4C3Tx, but we conduct thermal analysis to understand the physical limitations because there is not much research behind Nb4C3’s thermal properties.