## Slide 1
Structural and Morphological Characteristics of Rare Earth Element based MAX Phase and MXene
Joshua Abbott1, Vanessa Morris 1, Menuka Adhikari1, Sangeetha Balabhadra1, Alex Bretana2, Binod Rai2, Daniel Autrey1, Bhoj Gautam1
1Department of Chemistry, Physics and Materials Science, Fayetteville State University, Fayetteville, North Carolina 28301, United States
2Savannah River National Laboratory, Aiken, South Carolina 29808, United States
Figure 4. Morphology and elemental analysis of (Mo2/3Er1/3)2AlC MAX phase and (Mo2/3Er1/3)2C MXene
Summary
References
[1] L. Verger et. al., Curr. Opin. Solid State Mater. Sci., 23 (2019) 149-163.
[2] M. Khazaei et. al., Phys. Rev. Mater., 2 (2018) 074002.
[3] Y. Gogotsi, B. Anasori, ACS Nano. 13 (2019) 8491-8494.
[4] W. Wang et. al., Science. 379 (2023) 1242-1247.
(Mo2/3Er1/3)2C MXenes was synthesized using mild etching method.
The shifting and broadening of the (002) peak to lower angle was observed in MXenes compared to MAX phase.
The 39° 2θ peak related to aluminum is relatively small as in Mxenes relative to MAX phase.
More slate/sheet like structures were observed in (Mo2/3Er1/3)2C MXene compared to its MAX counterpart.
Atomic mass percentage of aluminum in (Mo2/3Er1/3)2AlC MAX phase is ~9% whereas it is below 1% after LiF/HCl Etching.
Contact Information:
Dr. Bhoj Gautam, Department of Chemistry, Physics and Materials Science
Fayetteville State University, Fayetteville, NC-28301
Email: bgautam@uncfsu.edu, Phone: 910-672-1653
a
b
a
b
Abstract
In this work, the MAX phase with a nominal composition of (Mo2/3Er1/3)2AlC was synthesized using conventional arc melting in an argon atmosphere with a water-cooled copper hearth. (Mo2/3Er1/3)2C MXene was synthesized by adding (Mo2/3Er1/3)2AlC powders into the LiF/HCl solution and was etched for 7 days and washed using HCl and deionized water. The resulting product was vacuum dried to remove any solvent residue. Structural, morphological, and elemental characterization was carried out using X-ray diffractometer and scanning electron microscopy (SEM). The lowest Bragg peak of the (Mo2/3Er1/3)2AlC powder was shifted to towards smaller angle and the 39° 2θ peak related to aluminum is relatively small as compared to (Mo2/3Er1/3)2AlC. These results indicate the successful extraction of aluminum atoms from (Mo2/3Er1/3)2AlC. These results are further supported by energy dispersive spectrometry (EDS) measurements. Our results provide important information regarding the structural and morphological characteristics of rare earth element based i-MXenes which dictate the optoelectronic, magnetic, and electrochemical properties of these materials.
Introduction
Sample Preparation:
Mild etching method
7 days at 70°C
Constant stirring
Oil bath
The resulting products were washed using HCl and deionized water, and vacuum dried at 70 0C to remove any solvent residue.
XRD Results
Figure 2. Photographs of etching, and decantate and prepared (Mo2/3Er1/3)2C Mxene ( left to right).
.
There has been a tremendous effort for the synthesis of crystalline MAX phases—a family of transition metal carbides and nitrides with a chemical formula of Mn+1AXn, where M is an early transition metal, A belongs to groups XIII – XVI in the periodic table, X is either C or N, and n can be in between 1 and 3 [1]. These materials have shown thermal and electrical conductance and have low density and high stiffness which open broad aspects of practical applications. Recently double transition metal MAX phases (M’2/3M’’1/3)2AX - out-of-plane ordered, labeled as o-MAX and in-plane ordered, labeled as i-MAX, were reported [1,2]. However, there are few reports on the synthesis and characterization of i-MAX and the corresponding MXenes. In this work, we synthesized Molybdenum-based rare earth containing i-MAX phase using arc melt technique. We then removed “A” element of i-MAX phase by acid treatment and sonication which resulted in two-dimensional (2D) transition metal carbides called MXenes [3]. These MXenes offer high conductivity, hydrophilicity, magnetism, good dispersion ability in solvents, mechanical stability, and structural diversity with at least 100 stoichiometric MXene compositions and are recognized as multifunctional materials [4].
Materials
Figure 1. Chemical structure of (Mo2/3Er1/3)2AlC MAX phase and (Mo2/3Er1/3)2C Mxene. −F is a functional group introduced after LiF/HCl etching.
Morphology and Elemental Analysis
Figure 3. XRD patterns of (Mo2/3Er1/3)2AlC MAX phase and (Mo2/3Er1/3)2C MXene. The vanishingly small 39 peak indicates the successful removal of Al from (Mo2/3Er1/3)2AlC MAX phase. The broadening of the (Mo2/3Er1/3)2C MXene peaks indicate that
the MXene is amorphous. The shifting of the (002) peak to lower values indicates an increase in the interlayer separation (c-parameter).
Acknowledgements
The synthesis of i-MAX phase and characterization work was supported by DOE BES-RENEW award number DE-SC0024611.This work was also partly supported by NSF RIA EES 1800795 for MXene synthesis.
(Mo2/3Er1/3)2AlC
(Mo2/3Er1/3)2C
Etching